## Slide 1
Molecular Structure Imaging and
Site-resolved Analysis
by Cs-corrected STEM
M. Haruta, H. Kurata
Institute for Chemical Research, Kyoto University, Uji, Kyoto, Japan
and S. Isoda
Institute for Integrated Cell-Material Sciences (iCeMS),
Kyoto University, Yoshida-Ushinomiya, Kyoto, Japan

## Slide 2
Institute for Integrated Cell-Material Sciences (iCeMS)
Founded October 2007
Kyoto University
World Premier International Research Center Initiative
by MEXT Japan;
“Globally visible” research centers.

## Slide 3
Interaction of cells and materials at mesoscopic domain

## Slide 4
Today’s outline
Cs correction for electron microscopy
STEM imaging with Cs correction for organic molecule
Site resolved STEM-EELS with Cs correction for brownmillerite
Cs; Spherical aberration
STEM; Scanning transmission electron microscopy
EELS; Electron energy-loss spectroscopy

## Slide 5
Short historical background of
high resolution imaging
TEM design sketch
The first TEM
(restored by Ruska in 1980)
The first TEM by E. Ruska and M. Knoll in 1931
Optical and electron microscopy images at 12 mag.

## Slide 6
100
(nm)
10
1
0.1
TEM; High voltage
TEM; Optimizing lens
Improvement of spatial resolution (point-to-point)
TEM
STEM
Cs; Spherical
aberration
TEM & STEM; Cs correction
Resolution has reached at 0.05 nm recently.
Resolution

## Slide 7
In 1979, high-resolution TEM was successfully applied to take atomic images in Cl16-CuPc by N. Uyeda.
Chemica Scripta, 14, 47-61, (1979)
Can ADF-STEM be applied for organic materials?
There have been no application of ADF-STEM to organic materials.
STEM has been believed to be inconvenient for taking images of organic materials, because of its strongly focused beam.
From TEM to STEM
TEM image

## Slide 8
2.6 nm
Image variation in HR-TEM
Computer simulated images for 1000kV
Scherzer focus
-100 nm -80 nm -60 nm
-40 nm -20 nm 0 nm
20 nm 40 nm 60 nm
The TEM images are very much variable depending on focus and thickness owing to the interference in TEM, because of the coherent imaging.
not quantitative,
almost no contrast of light elements
too sensitive to experimental conditions.
Notes: This shows an image taken for chlorinated-Cu-phthlocyanine thin crystal.
In the image, you can identify the atoms in the molecule, especially heavy atoms of Cu and Cl.

However, the TEM image depends largely on the value of defocus as shown in these image-simulations at different defocus values,
and the most reliable image is produced only at the Scherzer focus due to coherent interference of scattered electron waves.
This special defocus is originated from the spherical aberration.

## Slide 9
Transmitted wave
Diffracted waves
Objective lens
Probe scanning
Specimen
(Atomic arrays)
High angle scattered electrons by TDS at wider than 50 mrad
Scanning coils
High Angle Annular Dark Field (HAADF) image 【incoherent】
Bright-Field (BF) image 【coherent】
above 50 mrad
to collect only TDS
Low Angle Annular Dark Field (LAADF) image 【coherent+incoherent】
below 50 mrad
・High resolution
・Z-contrast (≈Zn), atomic structure
・EELS analysis
However, it is usually more difficult to take images of radiation-sensitive specimens than TEM.
ADF-STEM
(Annular Dark-Field Scanning Transmission EM)
50
30
100
(mrad)
Si
As
Si
As
Atomic scattering
Atomic scattering
TDS
TDS
Stronger TDS, but some contribution from elastic.
LAADF HAADF
Notes: As; arsenic , Si; silicon
As you know, HAADF-STEM of ADF-STEM creates images by collecting high-angle scattered electrons, typically above 50 mrad.
In this case, the scattering is originated by TDS, which realizes high resolution imaging with Z-contrast.
This provides us quantitative analysis of atomic structure.
However, it is usually more difficult to take images of radiation-sensitive specimens than TEM.
We notice eventually another imaging of ADF-STEM, that is LAADF-STEM as an alternative method.
As shown in this scattering profiles, above 50 mrad, the scattering happens mainly by TDS.
Since LAADF-condition below 50 mrad gives strongest TDS than HAADF-condition, it would be more suitable for imaging of radiation-sensitive materials.
But, in this case, one needs to be careful in interpretation of images taken because the images contain some contribution from elastically scattered electrons.

## Slide 10
Quantitative LAADF images ?  Yes
Intensity profiles
Cu
Cl
Cl
Experimental image
(a)
(b)
(c)
Simulated image
b-axis
a’-axis
Intensity ratio between Cu and Cl columns is 2.5.
↓
I ∝Z1.7 dependence
Notes: Intensity is proportional to Z to the power 1.7

## Slide 11
LAADF-STEM image (Cl8Br8-CuPc)
Particularly strong damage
at the lower image
6 M mag
Problems in STEM
Radiation damage, low magnification
1st scan
2nd scan
3rd scan
low mag

## Slide 12
Imaging condition (6,000,000 mag)
Probe size : 0.18 nm (FWHM)
Probe current : 5 pA
Dwell time : 60 msec/pix
Pixel size : 0.05 nm
Dose : ~ 12 C/cm2
0.18 nm
STEM probe
~ 0.35 nm
Probe size on scan area
In order to decrease the damage,
a finer probe is required.
pixel size < probe size
(over sampling)
The lower image part is particularly damaged.
0.05 nm
Pixels irradiated before the probe arriving.
Scan
direction
Probe position
FWHM
0.35 nm
Radiation damage due to the broadening of the incident beam

## Slide 13
In optical microscopes and commercial photo cameras, the spherical aberration has been compensated by combining the concave and convex lenses.
However, in electron microscopes (convex lens), there were no way to overcome the aberration until recently.
A factor to prevent to form a fine probe;
Spherical aberration
Cs correction  Fine probe  Low damage & high magnification
Notes: This shows again how does the spherical aberration affect the image formation.
All rays could not come onto a Gaussian image plane, but instead a relatively sharp image is formed at the defocus of Scherzer (least confusion).
The spot size at the least confusion determines the resolution of image.

## Slide 14
Aberration correction
Maximilian Haider, Stephan Uhlemann, Eugen Schwan,
Harald Rose, Bernd Kabius & Knut Urban;
“Electron microscopy image enhances”.
Nature, 1998;392:768-769. doi:10.1038/33823
Produce negative spherical aberration
Combine with positive aberration
Give a total of zero spherical aberration
＋
||
Multipole lenses.
http://www.superstem.org/cs-correction

## Slide 15
JEM 9980TKP1
Incident energy : 200 keV
Convergent semi-angle : 23 mrad
Spherical aberration : −0.025 mm
Fifth order spherical aberration : 15 mm
Probe size : 0.07 nm (FWHM)
ADF Detection angle : 39-104 mrad
ABF Detection angle : 11-23 mrad
EELS detection angle : 10 mrad
Probe current : ＜1 pA
Dose : ＜ 2.4 C/cm2
Cs-Corrector
Cs-corrected STEM in Kyoto Univ

## Slide 16
Spatial resolution ~ 0.18 nm
Less damaged, higher magnification 
Detectable images of N and C, but weak.
Observation at 25 M mag.
(scan step = 0.01 nm）
filtered images
Cs-corrected LAADF-STEM image
White contrasts are atoms

## Slide 17
Cs-corrected STEM + ABF-STEM
(Annular Bright-Field
Scanning Transmission Electron Microscopy)
LAADF
（detection angle≧20 mrad）
ABF
（detection angle =12 - 23mrad）
Direct Beam
α = 23 mrad
specimen
beam scan
More mixture of coherent and incoherent imagings.
Notes: 17

## Slide 18
Profiles in TEM and STEM
TEM
STEM
Slightly better in contrasts

## Slide 19
Possible to observe light elements in organic crystals by using Cs-corrected STEM, particularly combined with ABF-STEM,
due to increase S/N ratio, decrease radiation damages.
Unfortunately, this can be applied only for a few molecules with tough structure for strong electron bombardment.
Short summary on imaging
 Application of Cs-correction for site-resolved EELS analysis.

## Slide 20
Cs corrected STEM-EELS method
FeO6 octahedra and FeO4 tetrahedra
in the Sr2Fe2O5 and Ca2Fe2O5
 detection of local chemical bonding
relating to periodic oxygen deficiency
3. Summary
JAP, 110, 033708 (2011)
O K-edge ELNES of
FeO6 octahedron and FeO4 tetrahedron
in the brownmillerite
by using site-resolved STEM-EELS
with Cs corrector

## Slide 21
Principle of STEM-EELS method
(Scanning transmission electron microscopy
with electron energy-loss spectroscopy)
Energy Analyzer
Electron Energy-Loss Spectroscopy
（Elemental and state analyses）
Scan
Gun
Aperture
Illumination lens
Specimen
Annular detector
High-Angle Annular Dark- Field (HAADF) Image
（Structural analysis）
High angle scattered electrons
Elastically & inelastically scattered electrons
Scan coil
0.135 nm
HAADF of Si <110>
EDXS
(X-ray analysis)
Notes: This figure shows the principle of STEM-EELS method.
In STEM, the finely focused electron probe is scanned on a sample surface and the electrons scattered to the high angular region are detected by an annular detector. This signal is acquired from each scanning point to form an image, which is called high-angle annular dark-field imaging.
From this image, we can do the structural analysis of local area.
On the other hand, the energy of electrons scattered in small angular region are measured to obtain the EELS, which is used for elemental and state analyses.
HAADF and EELS signals can be acquired simultaneously, because of the different detection angle.
If the spectra are measured from each scanning point, we can construct elemental maps.
21

## Slide 22
① zero loss
② valence-electron excitation
③ core-excitation
EELS (Electron Energy-Loss Spectroscopy)
Core-loss spectrum
Chemical composition analysis
Partial Density of State (PDOS) of unoccupied band  chemical properties
Value of energy-loss and its intensity
Energy-Loss Near Edge Structure
(ELNES)
Extended Electron Loss Fine Structure
(EXELFS)
Radial distribution function
incident electron
 excitations
Inelastic scattering
Notes: And then,
This is a schematic diagram of EELS.
By using Core-loss spectrum, we can analyze these things
Especially, ELNES is related to the transition from atomic core state to the unoccupied state lying above the Fermi level,
which reflect the nature of chemical bonds around the excitation atom.
22

## Slide 23
Elemental mapping
“STEM-EDX chemical mapping of In, As and Ga”.
Ming-Wen Chu, Cheng-Hsuan Chen; PRL 104, 196101 (2010)
Red : Fe
Green : Ti
Blue : Sr
interface
Sr2Fe2O5
SrTiO3
EELS Elemental mapping of Sr2Fe2O5 / SrTiO3
 Electronic state mapping

## Slide 24
Ca(Sr)２Fe2O5 (Ca(Sr)FeO2.5)
Antiferromagnet : type G
TN = 720 K, 700 K for Ca, Sr
Acta Cryst. B 31, 641 (1975)
O1
O2
O3
layer structure
3 kinds of oxygen atom
a = 0.566850 nm
b = 1.55823 nm
c = 0.52653 nm
Brownmillerite oxide
Orthorhombic
Space group : Icmm
SrFeO2.5
a = 0.5946 nm
b = 1.48273 nm
c = 0.54307nm
Brownmillerite oxide
Orthorhombic
Space group : Pcmn
CaFeO2.5
including a randomly-oriented tetrahedral chains
 calculation for Ibm2
FeO4 tetrahedron
FeO6 octahedron
b
a
Notes: In the present research,
Our aim is to investigate the local electric structure using site resolved EELS spectrum for brownmillerite structure of Sr2Fe2O5 .
Crystal structure for bulk crystal are indicating here.
In this crystal, the FeO6 octahedra and FeO4 tetrahedra are arranged in layers.
Therefore , there are 3 kind of oxygen atom in the unit cell.
And this is antiferromagnetic material type G.
Sr2Fe2O5 thin film can be grown on SrTiO3 substrate using pulsed Laser Deposition.
24

## Slide 25
1.94Å
2.217Å
1.82Å
2.04Å
Distortion of FeO6 octahedra, even though non Jahn-Teller ion of Fe3+ ?
Effect of substitution Ca by Sr ?
Understand the origin of the distortion by using site-resolved ELNES, mainly examined by O K-edge.
Aim
Simulation WIEN2k + TELNET.2;
Full-potential linear augmented pale wave plus local orbital (LAPW+LO) method.
Spin-polarized generalized-gradient approx. for exchange-correlation potential.
Core-hole is included.
CaFeO2.5

## Slide 26
Substrate | SrTiO3 (001)
Substrate temperature | 800℃
Oxygen pressure | 1.0E-5 Torr
Laser fluence | 101 mJ
Laser repetition rate | 10 Hz
Film thickness | 120 nm
PLD (Pulsed Laser Deposition)
SrFeO2.5
CaFeO2.5
Solid state stoichiometric reaction of CaCO3 and Fe2O3
Sample preparation

## Slide 27
W-filter
Double tank
CCD camera
Nanotip-FEG
Cs corrector
Nanotip cold-FEG (field-emission gun)
・Acceleration voltage：200 kV
・Emitter：W<111>
・Build-up of emitter：Thermal-field treatment
・Pressure： < 5 x 10-9 Pa
Cs corrector
・Convergent semi-angle：23 mrad
・Probe size：0.07 nm
Omega filter
・Energy resolution：0.4～0.5 eV
・Collection angle：10 mrad  dipole transition
HAADF-STEM
Detection angle : 70 - 170 mrad
Cs corrected STEM equipped with a nanotip FEG
ABF-STEM ;
JEM-ARM200F (200 kV, detection angle= about 11.5 – 23 mrad)
Notes: The experiment was performed using this microscope.
The spherical aberration corrector is incorporated, which forms the fine electron probe less than 0.1 nm in diameter.
EELS spectrum is measured by an omega type of filter.
The energy resolution is 0.4 to 0.5 eV owing to the cold field emission gun.
27

## Slide 28
ABF-STEM image of SrFeO2.5 [101] projection
octa
hedral
tetra
hedral
HAADF-STEM
ABF-STEM
stronger
weaker due to de-channeling
Shift of O
0.5 nm
0.5 nm
HAADF-STEM
ABF-STEM
b
Probe electron

## Slide 29
Delocalization of EELS events
delocalization
Limit of spatial resolution.
Cs correction, so as not to make worse more.
Coulomb interaction with nucleus  point-like
elastic scattering
inelastic scattering (core-loss)

## Slide 30
0.5 nm
To keep the probe minimum by Cs correction.
Delocalization

## Slide 31
dE =
2θE3/4
λ
= 0.18 nm for O, 0.14 nm for Fe
θE =
2・E0
ΔE
=
2・200・103
530 or 710
= 1.325 mrad for O, 1.775 mrad for Fe
Delocalization and Scanning
0.18 nm
0.14 nm
O1
O2
O3
HAADF-STEM image ［101］
Sr
Sr
Sr
Sr
Sr
Sr
Fe
Fe
［101]-projection model
Beam was scanned on Fe sites, so as to avoid damage.
ELNES of O K-edge
5 nm
Characteristic angle
Notes: In order to realize the site-resolved EELS spectrum,
delocalization for inelastic scattering electron is important.
Delocalization means that spatial distribution for EELS signal.
And the delocalization can be defined as this equation.
Looking at the distribution of delocalization for oygen atom along the [101] projection.
It is theoretically expected that the site-resolved EELS is possible when the electron probe put on the Fe site.
This is a typical HAADF-STEM image of Sr2Fe2O5.
we can easily distinguish the octahedra site and tetrahedra site from the image contrast.
Experimentally EELS spectra were acquired by scanning the electron probe on the each equivalent Fe site.
４分～15秒
31

## Slide 32
O K ELNES of CaFeO2.5 and SrFeO2.5
Experimental (blue solid line) and calculated (red dotted line) O K-edge ELNES of (a) CaFeO2.5 and (b) SrFeO2.5 measured over the whole unit cell, and at the individual FeO6 octahedral and FeO4 tetrahedral sites.
Basically both spectra are very similar.
Pre-peak-A; from O 1s to unoccupied O 2p hybridized with Fe 3d near Fermi level.
significantly different for tetra (non-split) and octa (split)
 splitting of Fe 3d band by crystal field.
Peak-B and Peak-C; to unoccupied O 2p with Ca(Sr) 3d(4d) and Fe 4s/4p, respectively.
In simulation, all relevant oxygens in delocalization are included.

## Slide 33
Spin-polarized Fe1-3d DOS
Ground state calculation
dxy, dyz and dzx
dz2
dx2-y2
ELNES splitting ;
distortion in FeO6 octahedron from cubic by periodical ordered oxygen vacancy as observed in ABF-STEM.
Schematic crystal-field splitting
3 peaks
Simulation for CaFeO2.5
without orientation disorder.
If 5 electrons in Fe1 is up-spin at occupied band, strong down-spin at unoccupied one.

## Slide 34
Spin-polarized partial DOS of CaFeO2.5 at the ground state.
Unoccupied Fe 3d-DOS at (a) the Fe1 octahedral site, and (b) the Fe2 tetrahedral site.
Unoccupied O 2p-DOS at (c) the O1 site, (d) the O3 site, and (e) the O2 site.
antiferromagnetic of Type-G
Super-exchange interaction (e.g. Fe1 and Fe2 through O2)
Asymmetry for up- and down-spin bands of O2.
Whole spin-polarized Fe 3d- and O 2p-DOS

## Slide 35
1s
1s
1s
Ground
state
Transition
state
Excited
state
EF
1 hole
0.5 hole
no hole
Core-hole effect in simulation
real final state
O K-edge
DOS of electron
O-1s
Simulation WIEN2k + TELNET.2 ;
Full-potential linear augmented pale wave plus local orbital (LAPW+LO) method.
Spin-polarized generalized-gradient approx. for exchange-correlation potential.
Core-hole is included. for a primitive cell
EF
A-atom
B-atom
Notes: There are some experimental investigations of local electronic structures at internal interfaces and defects such as dislocations. It is, however, hard to analyze directly the local electronic state from an experiment, so we need to simulate ELNES from a model to say something about p-DOS of specimens.
So far, unfortunately, we had no appropriate simulation tools to understand fine structures correctly, because so-called core-hole effect should be taken into account in the calculations. The core-hole effect is an effect changing electronic states due to hole-formation in deep energy level after excitation. The core-hole effect requires us to perform calculation in a larger unit cell so as to avoid artificial interaction between excited atoms.
Recently, owing to the development of calculation techniques, the ELNES can be simulated by first principles band calculations, which providing a better understanding of the local electronic structures. There are several methods to incorporate the core-hole effect in the calculation. From our experience, the best agreement with the experimental spectrum was achieved with the excited state calculation. That is fully excited approximation as shown here schematically.
( This figure shows the three types of calculation including a core-hole effect together with ground state calculation disregarding the core-hole effect,
that is, the excited state calculation with a 1s core-hole, Z+1 approximation with an introduction of Al instead of Mg (not shown in the slide), and the transition state calculation with a half of core-hole. )

## Slide 36
Large shift toward EF;
dz2, dyz, dzx
Fe2 3d DOS depends on location site of core-hole.
These changes come from different screening of core-hole potential at each O site
Unoccupied 3d-DOS with core-hole
for down-spin at octahedral Fe1
Smaller shift;
dx2-y2, dxy
Core-hole on O2
Core-hole on O1

## Slide 37
Individual spin-polarized O K-edge ELNES
Simulation WIEN2k + TELNET.2
As a result, the peaks A1, A2, and A3 (blue line) in the pre-peak region.
 The transitions to the O 2p band hybridized mainly with the Fe1eg/b2g, b1g and a1g states, respectively.
assuming Ibm2 symmetry for SrFeO2.5
without orientation disorder.

## Slide 38
O K-edge ELNES simulation
from PDOS with core-hole
O3
O2
O1
O1&O2
O2&O3
The pre-peak splitting of the experimental spectra at the octahedral site
The local electronic structure of the Fe-3d band around the distorted FeO6 through hybridization between the O 2p and Fe 3d bands.
In contrast, the crystal field splitting at the FeO4 site is smaller.
Here the oxygen atom (O2) linking FeO6 and FeO4 contributes to both site-resolved spectra.
The simulation can explains well the specific features of ELNES.

## Slide 39
What is happening in CaFeO2.5
Pre-peaks  not purely ionic, but some covalent.
The integrated intensity of the pre-peak of O2;
up-spin spectrum > down-spin spectrum,  Asymmetric interaction
The number of holes in the O2 2p band hybridizing with the 3d band of;
tetrahedral Fe2 site > octahedral Fe1 site
indicating that charge transfer;
from O2 to Fe2 > from O2 to Fe1  asymmetrical charge transfer
 covalent nature of Fe2-O2
 shorter bond length (distortion) of Fe2-O2
 distortion in FeO6 octahedron

## Slide 40
Experimental Fe L2,3-edge ELNES of CaFeO2.5
(a) the whole unit cell, and at the (b) FeO6 octahedral. and (c) FeO4 tetrahedral sites.
0.5 eV
The Fe1 octahedral site is similar to a typical Fe3+ spectrum from hematite, which shows a shoulder peak at the low energy side of the L3 peak.
The transition energy from the Fe 2p level to the Fe 3d band is lowered at the Fe2 tetrahedral site by the increase in Coulomb repulsion between the 2p electrons and valence electrons due to charge transfer from O2.
Different amounts of valence charge are localized at Fe1 and Fe2 ions, as shown by calculation.
Fe2
Fe1

## Slide 41
Story for SrFeO2.5
Total intensity is nearly the same for Fe1 and Fe2.
larger in O3
small in O1
By substitution from Ca to Sr,
larger charge transfer from O3 to Fe2.
Tetragonal site has stronger covalent than that in CaFeO2.5
and then shorter length of Fe2-O3.
Result into big difference in bonding of Fe2-O3 and Fe2’-O3.
SrFeO2.5
CaFeO2.5
Different for Fe1 and Fe2.

## Slide 42
The site-resolved ELNES was applied to FeO6 octhahedra and FeO4 tetrahedra in Sr(Ca)FeO2.5 crystal.
The splitting observed in the pre-peak of the O K-edge, indicating transition to an unoccupied O-2p band hybridized with the Fe-3d band, demonstrated the strong crystal field of the octahedral site as compared to the tetrahedral site.
The charge transfer from O2 to the tetrahedral Fe2 atom is larger than that to the octahedral Fe1 atom in Ca(Sr)FeO2.5.
The bonding character between O2 and the tetrahedral Fe2 atoms is more covalent than that between the O2 and Fe1 atoms, which leads to the observed difference in bond length between O2-Fe2 and O2-Fe1.
Asymmetrical charge transfer at the O3 atom linking the tetrahedral Fe atoms in SrFeO2.5. The difference in bond length between O and the tetrahedral Fe atoms in the ac plane was caused by an asymmetrical charge transfer.
Summary
Notes: 以上まとめますと、
42

## Slide 43
Acknowledgements
This work was partly supported by Grants-in-Aid for Scientific Research Grants Nos. 19GS0207 and 19310071 and for JSPS Fellows No. 20–145 from MEXT (Ministry of Education, Culture, Sports, Science and Technology, Japan).
Mr. Kawasaki, Dr. Otsuka and Ms. Nishimura of TRC for preparing the cross-section samples.
Dr. Okunishi for observing the ABF images with 200 kV microscope (JEM-ARM200F) in JEOL company.
Notes: 43

## Slide 44
Than you for your kind attention
Dr. M. Haruta
Prof. H. Kurata
Finally, really have to say that I would like to express the appreciation from the people of Japan for your enormous supports on the occasion of terrible earthquake in eastern Japan in this March.

## Slide 46
Elastic cross-section ；sel
Inelastic ；sinel
Backscattering ；sp/2
Ionization ；sk
Knock-on ；sd
L. Reimer; “Transmission Electron Microscopy”, Springer-Verlag
Radiation damages of organic and inrganic materialsa
（difference in oraganic or carbon materials）
Change in electronic states
(Ionization)
Displacement of atoms
(Knock-on)
100 keV

## Slide 47
3.11 Huge earthquake in eastern Japan
flooded near Sendai–city,
about 5 km from seashore
quake distribution (震度分布)
max quake > 7
仙台市
相馬市
Mw=9.0

## Slide 48
義援金; 150億円以上
Helping hand from Taiwan
Our future issue
感謝來自台灣的援助
Nuclear Power Station in Fukushima
在福島核電站
Notes: First of all, really have to say that I would like to express the appreciation from the people of Japan for your enormous supports on the occasion of big earthquake in eastern Japan in this March.

## Slide 49
Members of iCeMS

## Slide 50
Graphical examples

## Slide 51
High voltage TEMs in Kyoto University
Shimadzu 300kV, 1957
Shimadzu 500kV, 1964
JEOL 500kV, 1971
JEOL 1000kV, 1989
Shorter wavelength realizes better resolution.
 High voltage TEMs
Notes: This shows our own history on improving high voltage electron microscopes.
About 50 years ago, Kyoto University started high voltage electron microscopy which accelerating voltage increased up to 1MV.
The main aim is to improve the resolution by using shorter electron wavelength.
Another aim was to decrease the radiation damage, in particular for organic, polymeric and biological specimens.
The damage could make smaller due to lower cross-section for high voltage electron beam.
However, at the same time, detection efficiency of detector became worse due to again the lower cross-section, even when we employed various detectors; such as high sensitive photographic films, image intensifier, imaging plate and CCD camera.

## Slide 52
Microscopy by lens or scanning
1. Microscopy with lens | 2. Scanning microscopy
Conventional optical microscopy TEM | Scanning probe microscopy (AFM, STM) SEM, STEM
Incident beam
Image
Lens
Sample
Incident probe
Sample
Transmitted signals
Scan
Output signals

## Slide 53
W-filter
Double tank
CCD camera
Nanotip-FEG
Cs corrector
Nanotip cold-FEG (field-emission gun)
・Acceleration voltage：200 kV
・Emitter：W<111>
・Build-up of emitter：Thermal-field treatment
・Pressure： < 5 x 10-9 Pa
Cs corrector
・Convergent semi-angle：23 mrad
・Probe size：0.07 nm
Omega filter
・Energy resolution：0.4～0.5 eV
・Collection angle：10 mrad
Cs corrected STEM equipped with a nanotip FEG
Stability : 0.2 nm/min (spatial)
0.04 eV/min (energy)
Notes: The experiment was performed using this microscope.
The spherical aberration corrector is incorporated, which forms the fine electron probe less than 0.1 nm in diameter.
EELS spectrum is measured by an omega type of filter.
The energy resolution is 0.4 to 0.5 eV owing to the cold field emission gun.
53

## Slide 54
基板
a
26.5°
c
Monoclinic (C2/c)
a = 1.962 nm
b = 2.608 nm
c = 0.376 nm
β = 116.5°
Critical dose ≈ 30 C/cm2
HR-TEM for an organic crystal
of phthalocyanine
electron beam
Crystal structure of Cl16CuPc;

## Slide 55
AFM image
carbon support layer
1
3
2
4
・Vacuum-deposition on a cleaved KCl (001)
・Pretreatment of substrate at 670 K for 1 hr
・Deposition at 590 K
・Thickness measurement by AFM (30-49 nm)
・Thin support layer by carbon deposition
・Floating off from the substrate on water
quartz crucible
Mo-wire heater
shutter
substrate
heater
thermocouple
quartz oscillator
TMP
30nm
EM specimen preparation
AFM

## Slide 56
Previous TEM images of the phthalocyanines
1958 Menter
1970 - 79 Uyeda, et al.
1993 Kobayashi, et al.
No molecular image.
but lattice image of 1.3 nm.
improved atomic image
Molecular image
Notes: This shows the improvement of such images.
At present, one can see directly the molecular arrangement in a crystal and even atomic arrangement in the molecule.

## Slide 57
Cs-corrected HR-TEM image
高分解能分子像（フタロシアニン分子）
HR-TEM Image taken at 1000 kV
Recent improvement in TEM imaging

## Slide 58
Camera length of 12cm in JEOL 2200FS (detection angle of 20～53 mrad); LAADF-STEM condition
The Z-contrast HR could be expected even in LAADF-condition.
The higher TDS intensity can be used for imaging so as to minimize radiation damage.
Diffracted waves
LAADF detector
For organic crystals, diffracted waves are concentrated at lower angles due to their large lattice dimensions.
Small contribution from elastic.
CBED-pattern
Inner diameter of LAADF detector of 12 cm
LAADF-STEM observation
of organic materials
Notes: We adopted the camera length of 12 cm as a LAADF-STEM condition in JEOL 2200FS, which corresponds to the detection angle of 20～53 mrad);
For the typical organic crystals, diffracted waves are concentrated at lower angles due to large lattice dimensions.
In such cases, the elastic contribution might be small, so that the high resolution could be expected even in LAADF-condition.
Of course, highest TDS intensity can be used for imaging so as to minimize radiation damage.

## Slide 59
a = 19.49Å
b = 25.96Å
The critical dose is about 30 C / cm2
Crystal structure
monoclinic
a = 1.949 nm b = 2.596 nm
c = 0.376 nm β = 116.5°
substrate
a
26.5°
c
Cl16-CuPc
SAED
a=1.962 nm, b=2.604 nm, c=0.376 nm, b=116.5 °
a=1.962 nm
b=2.604 nm
electron beam
Notes: Firstly, I would like to present the usefulness of LAADF-STEM for molecular imaging.
The specimen is C16-CuPc whose critical dose is about 30 C/cm2.
The electron beam is introduced along its c-axis.
And these kind of image is expected.

## Slide 60
Objective lens
Sample
(atomic columns)
Scan coil
(High-Angle Annular Dark-Field Scanning Transmission Electron Microscopy)
Annular detector
Scattering angle (mrad)
Intensity
Si単原子からの弾性散乱波とTDS波
TDS
elastic
Debye-Waller factor : 0.5Å2
0
50
100
150
200
0.05
0.10
0.15
0.20
0.25
0.30
0.00
【coherent】
Ratherford scattering
High order diffraction【incoherent】
Thermal diffuse
scattering (TDS)
s=sin(θ)/λ,
fx(s) ; the atomic structure factor for electron
Mx(s) =Bs2; the temperature factor of each element x
B ; Debye-Waller factor
detect a range larger than 50 mrad
HAADF-STEM
High angular scattering electrons

## Slide 61
Chart: 
| 0 | 2.5000006510421251 | 5.0000052083479476 | 7.5000175782361911 | 10.00004166713542 | 12.50008138163887 | 15.0001406285597 | 17.500223314985629 | 20.000333348334181 | 25.000651087447292 | 30.0011251139215 | 35.001786704574513 | 40.002667146781 | 45.003797740236273 | 50.005209798722277 | 55.006934651874673 | 60.009003646953943
C_TDS | 0 | 0.15095 | 0.49394 | 0.71639 | 0.77955 | 0.6978 | 0.55897 | 0.42169 | 0.30722 | 0.15973 | 0.088803 | 0.048265 | 0.032385 | 0.019599 | 0.0144 | 0.01 | 0.0064
C_elastic | 6.0025 | 4.9566 | 3.8742 | 2.3112 | 1.2654 | 0.6247 | 0.28743 | 0.12591 | 0.052779 | 0.0083692 | 0.001197 | 0.00013527 | 1.4968e-05 | 1.1774e-06 | 8.8477e-08 | 4.9436e-09 | 2.0025e-10
N_TDS | 0 | 0.13034 | 0.41253 | 0.66784 | 0.79049 | 0.75979 | 0.6604 | 0.5305 | 0.4063 | 0.21893 | 0.12087 | 0.072696 | 0.04408 | 0.028898 | 0.0196 | 0.0121 | 0.01
N_elastic | 4.84 | 4.2797 | 3.2356 | 2.1546 | 1.2831 | 0.68021 | 0.3396 | 0.1584 | 0.0698 | 0.011471 | 0.0016292 | 0.00020374 | 2.0373e-05 | 1.736e-06 | 1.2043e-07 | 5.9818e-09 | 3.1289e-10
Cl_TDS | 0 | 0.45865 | 1.5226 | 2.5107 | 2.9474 | 2.8353 | 2.3975 | 1.8764 | 1.4331 | 0.7939 | 0.46309 | 0.28943 | 0.19328 | 0.13686 | 0.096096 | 0.0676 | 0.0529
Cl_elastic | 21.16 | 18.1175 | 14.4774 | 9.9502 | 5.9927 | 3.2656 | 1.6426 | 0.78048 | 0.36253 | 0.070995 | 0.013009 | 0.0021714 | 0.00032168 | 4.1555e-05 | 4.3629e-06 | 3.7582e-07 | 2.9486e-08
Cu_TDS | 0 | 0.53597 | 1.5207 | 2.2171 | 2.525 | 2.5937 | 2.525 | 2.3393 | 2.158 | 1.6787 | 1.1904 | 0.85479 | 0.58016 | 0.39382 | 0.26973 | 0.20236 | 0.14437
Cu_elastic | 42.25 | 35.464 | 24.5914 | 15.339 | 9.3086 | 5.7007 | 3.5266 | 2.1551 | 1.3389 | 0.48216 | 0.15518 | 0.047711 | 0.012744 | 0.0030762 | 0.00067025 | 0.00014238 | 2.5542e-05
Br_TDS | 0 | 1.1417 | 3.5993 | 5.5534 | 6.2959 | 6.023 | 5.2346 | 4.3788 | 3.587 | 2.3499 | 1.5688 | 1.0735 | 0.77311 | 0.53274 | 0.38438 | 0.2809 | 0.2025
Br_elastic | 53.29 | 45.0983 | 34.2232 | 22.0091 | 12.801 | 6.937 | 3.5863 | 1.8213 | 0.9074 | 0.21014 | 0.04407 | 0.0080542 | 0.0012867 | 0.00016176 | 1.7452e-05 | 1.5617e-06 | 1.1287e-07
Chart: 
| 0 | 2.5000006510421251 | 5.0000052083479476 | 7.5000175782361644 | 10.00004166713542 | 12.50008138163887 | 15.0001406285597 | 17.500223314985629 | 20.000333348334081 | 25.000651087447292 | 30.0011251139215 | 35.001786704574513 | 40.002667146781 | 45.003797740236273 | 50.005209798722277 | 55.006934651874673 | 60.009003646954113 | 65.011448150617611 | 70.014299550697899 | 75.017589257977903 | 80.02134870797785 | 85.025609362742401 | 90.030402712626753 | 95.035760278101748 | 100.0417136115406 | 105.0482942990343 | 110.05553396220181 | 115.0634642600016 | 120.0721168905559 | 125.0815235929828 | 130.09171614922181 | 135.10272638588609 | 140.11458617609989 | 145.12732744137119 | 150.14098215343321 | 155.15558233613669 | 160.17116006731749 | 165.18774748069339 | 170.20537676774629 | 175.22408017965569 | 180.2438900291865 | 185.26483869264581 | 190.28695861178011 | 195.31028229575989 | 200.3348423231196
elastic | 36 | 27.5985 | 19.1674 | 11.3694 | 6.4451 | 3.6458 | 2.1675 | 1.3385 | 0.88657 | 0.42647 | 0.2347 | 0.13533 | 0.076141 | 0.045553 | 0.026818 | 0.015775 | 0.0094771 | 0.0054236 | 0.00316 | 0.0018301 | 0.0010527 | 0.00060087 | 0.00034007 | 0.0001907 | 0.00010586 | 5.8143e-05 | 3.157e-05 | 1.6937e-05 | 8.9721e-06 | 4.6907e-06 | 2.4191e-06 | 1.2301e-06 | 6.1648e-07 | 3.0439e-07 | 1.4802e-07 | 7.0865e-08 | 3.3395e-08 | 1.5485e-08 | 7.0643e-09 | 3.1697e-09 | 1.3985e-09 | 6.0669e-10 | 2.5872e-10 | 1.0843e-10 | 4.4662e-11
TDS | 0 | 0.069083 | 0.19264 | 0.25871 | 0.26303 | 0.23513 | 0.20412 | 0.17443 | 0.15383 | 0.12113 | 0.1017 | 0.085571 | 0.068259 | 0.056847 | 0.046082 | 0.037125 | 0.030523 | 0.02397 | 0.019274 | 0.015534 | 0.012565 | 0.010211 | 0.0083433 | 0.0068586 | 0.0056742 | 0.0047252 | 0.0039611 | 0.0033423 | 0.0028383 | 0.0024252 | 0.0020844 | 0.0018016 | 0.0015654 | 0.0013669 | 0.0011992 | 0.0010568 | 0.00093505 | 0.00083058 | 0.00074047 | 0.0006624 | 0.00059447 | 0.00053513 | 0.0004831 | 0.00043731 | 0.00039687
Scattering angle (mrad)
Intensity
TDS
elastic
Debye-Waller factor : 0.5Å2
Scattering from isolated atom for 200kV
Application of ADF-STEM to organic crystals
Intensity
LAADF inner angle
Br
Cl
Cu
C
N
s=sin(θ)/λ,
fx(s) ; the atomic structure factor for electron
Mx(s) =Bs2; the temperature factor of each element x
B ; Debye-Waller factor
HAADF inner angle
Scattering angle (mrad)
Inorganic crystal
Organic crystal
Si
7

## Slide 62
ABF
(annular bright-field )
HAADF
Sr
Sr
Sr
Sr
Sr
Sr
Sr
Sr
Sr
Sr
Fe
Fe
Ti
SrTiO3
SrTiO3
Sr2Fe2O5
Sr2Fe2O5
Distortion of octahedron is visible in ABF image.
Reference : Haruta et al., Proceedings of EDGE2009, 64 (2009)
Sr
Sr
Sr
Sr
Ti
O
O
O
O
Sr
Sr
Sr
Sr
Sr
Sr
Fe
Fe
O
O
O
O
O
Notes: Recently, new imaging method using STEM is developing.
By using ABF image, we can observe oxygen columns.
For example, in case of STO, oxygen are observed in the center,
On the other hand, in case of SrFeO2.5, distorted octahedra are observed directly.
Therefore, the Distortion of octahedron is also confirmed using ABF image.
62

## Slide 63
Scott D. Findlay, Tomohiro Saito, Naoya Shibata, Yukio Sato, Junko Matsuda, Kohta Asano, Etsuo Akiba, Tsukasa Hirayama, and Yuichi Ikuhara
"Direct Imaging of Hydrogen within a Crystalline Environment"
Applied Physics Express 3 (2010) 116603
ADF
(HAADF)
ABF
ABF
filtered
Observation of hydrogen atoms !!

## Slide 64
Advantage of LAADF-STEM
for high resolution of organic crystal
M. Haruta, h. Kurata adn S. Isoda. Ultramicroscopy, 2008, 108, 545-551.
Cu
Cl
Cl
a’
b
・Z-contrasts of Cu- and Cl-columns are observed.
・C- and N-columns are not observed.
・First observation of ADF-STEM in organic materials.
a = 19.49Å
b = 25.96Å

## Slide 65
(f)
(g)
Beam size effect in STEM
Scherzer focus
slightly under focus
scanning
scanning
Pre-peak damages materials before imaging.

## Slide 66
Ultramicroscopy ,19, 279 (1986)
TEM image of stacking faults
in Cl16CuPc

## Slide 67
5.2Å
Stacking faults in Cl16CuPc

## Slide 68
O K-edge
Energy- loss (eV)
Whole unit cell
FeO6 site (oct)
FeO4 site (tetra)
Intensity (arb. unit)
Exp
Cal
O K-edge
occupied
unoccupied
Fe-3d
Sr-4d
Fe-4s/4p
O-2p
Dipole transition
Δl= ±1
O-2p hybridized with
Split & weak
for octahedron site
DOS of electron
O-1s
Notes: This is a result of O K-edge ELNES from each site.
O K-edge is transition from 1s band to unoccupied 2p band.
And the experimental spectrum from whole unit was agree well with the calculated spectrum
Site-resolved EELS is realized and
Each spectrum has different futures reflecting local electric structure.
By comparing with the theoretical PDOS result,
It was found that the each peak is attributed to these hybrid state.
Especially, pre-peak is most different.
The pre-preak in octahedra site is sprited, while that of in tetrahedra site is not sprited.
And the intensity of pre-preak in octahedra site is smaller than that in tetrahedra site.
This means the hole concentration in octahedra site is smaller than that of tetrahedra site.
It is considred ｔhese results reflect the nature of chemical bonding.
Transition metal oxide electronic properties are strongly related to the partially filled 3d
band of the transition-metal atoms, which are strongly hybridized with the O 2p bands.
The pre-peak has a strong Fe 3d band contribution and is extremely sensitive to bonding features.
68

## Slide 69
up + down
up
down
O-K edge of FeO4 site
Energy loss(eV)
FeO4 site
Exp
O1&O2
O1
O2
The crystal field splitting for FeO4 site was smaller than that of FeO6 site.
 more covalent nature ??? than FeO6
Intensity (arb. unit)
O3
O2
O1
Notes: While in case of the O K-edge of FeO4 tetrahedron site.
69

## Slide 70
Mangetic structure of Sr2Fe2O5
Energy loss (eV)
up + down
up
down
1.94Å
2.217Å
1.82Å
2.04Å
FeO6 site
Intensity (arb. unit)
O K-edge of FeO6 site
eg
t2g
x2-y2
(d )
3z2-r2
(d )
xy
(d )
yz
(d
zx
, d )
Fe-3d state
b1g
a1g
b2g
eg
O3
O2
O1
x2-y2
(d )
b1g
(d )
a1g
3z2-r2
Since the FeO6 octahedra is distorted by periodic oxygen defect, it was expected that such a distortion from cubic symmetry leads to a splitting of the t2g and eg states.
 pre-peak splitting
Notes: Since the FeO6 octahedra is distorted by periodic oxygen defect.
it was expected that such a distortion from cubic symmetry leads to a splitting of the t2g and eg states.
The b1g state is extended into the in-plane, while the a1g state is directed in the z direction
Therefore, a1g state make the stronger hybridization with O2 2p band than that of O3.
Therefore, it was found each pre-peak are attribute to these state.
70